## Slide 1
Side view
Top view
Si/SiO2 substrate
Notes: Si substrate

## Slide 2
Side view
Top view
Si/SiO2 substrate
magnetron cathode
N
S
S
target material (M)
deposited material (M)
Ar source
optional O2 source
high density plasma
target material atom
ionized Ar
negative voltage
Notes: Thin film deposition by means of megnetron sputtering. Optional oxygen flow may be enabled to deposit target material oxide (ex. MgO, Al2O3)

## Slide 3
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
Notes: MTJ stack with bottom buffer (metalic) and caping (metalic) fully deposited

## Slide 4
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
negative photo-resist
Notes: Negative photoresist is being aplied in spin coater (AR 7520.17) 6000 rpm@30s => 0.3um, baking 85deg@60s

## Slide 5
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
exposed photo-resist
moving electron beam
Notes: Photoresist is being exposed using electron beam lithography

## Slide 6
developer bath
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
exposed photo-resist
Notes: Photoresist is being developed using AR300-47 (120s), rinsed in di-h2o for 30s and baked in 85deg for 60s

## Slide 7
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
exposed photo-resist
accelerated argon atom
Notes: Sample is being etched using ion etching to form bottom electrode shape by reaching Si substrate. Mass spectrometer is being used to determine layers that are being etched

## Slide 8
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
exposed photo-resist
Al2O3
Al2O3
Notes: Al2O3 is being deposited to match etched height, using tehnique presented earlier (Al target and O2 injected near sample)

## Slide 9
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
Al2O3
remover bath
Notes: Photoresist is being removed together with excess Al2O3 in Sigma Aldrich (….?...) in ultrasonic bath

## Slide 10
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
Al2O3
negative photo-resist
Notes: Negative photoresist is being aplied in spin coater (AR 7520.17) 6000 rpm@30s => 0.3um, baking 85deg@60s

## Slide 11
Side view
Top view
Si substrate
bottom buffer
capping
MTJ layers
Al2O3
exposed
photo-resist
exposed
photo-resist
Notes: Photoresist is being exposed using electron beam lithography to form pillar shape (circle) and via shape (square)

## Slide 12
Side view
Top view
Si substrate
bottom buffer
exposed
photo-resist
exposed
photo-resist
Notes: After developing the resist, etching is performed to reach bottom buffer. Etching time is strictly controlled based on spectrometer signal. The pillar is formed.

## Slide 13
Side view
Top view
Si substrate
Al2O3
exposed
photo-resist
exposed
photo-resist
Notes: Again Al2O3 is deposited

## Slide 14
Side view
Top view
Si substrate
Al2O3
remover bath
Notes: Again photoresist and excess Al2O3 are removed

## Slide 15
Side view
Top view
Si substrate
Al2O3
positive photo-resist
Notes: Positive photoresist ARP 672.08 is applied in spin coater (6000 rpm@30s => 0.75um) and baked 150deg@3min

## Slide 16
Side view
Top view
Si substrate
Al2O3
exposed photo-resist
exposed photo-resist
Notes: Photoresist is being exposed using electron beam lithography to form top electrode shape

## Slide 17
Side view
Top view
Si substrate
Al2O3
developer bath
Notes: Resist is developed

## Slide 18
Side view
Top view
Si substrate
Al2O3
Al Al
Au Au
Al
Au
Notes: Al (as buffer) and then Au is deposited as a material for top electrode

## Slide 19
remover bath
Side view
Top view
Si substrate
Al2O3
Notes: Photoresist and excess Al/Au are removed (sigma)

## Slide 20
Side view
Top view
Si substrate
Al2O3
TOP CONTACT
BOTTOM CONTACT
MTJ pillar
VIA
Notes: Sample manufacturing is complete, having contacts to access both top and bottom electrode of the MTJ